**Trash Rack Requirements**

The Trash Racks are steel with bare ferrous metal surfaces given two (2) coats of Tnemec N69 Hi-Build Expoxoline II Primer applied at a rate that will provide a minimum Dry Film thickness of Four (4) to six (6) mils. Followed by one (1) topcoat of Tnemec 1075 Endura-Shield II applied at a rate that will provide a minimum dry film thickness of two (2) to five (5) mils.